Lattice resonant amplification in solids and Flash

Ric Fulop

Massachusetts Institute of Technology

ricfulop@mit.edu

30 December 2025

# Abstract:
Flash emerges when an external drive overwhelms intrinsic damping in a solid lattice, placing it in a resonant amplification mode. We show that high fields create a steady-state two-temperature condition where hot electrons resonantly amplify soft optical phonon modes. Once the pumping rate exceeds anharmonic decay, the resonant vibrational mode softens the lattice and collapses the migration barrier, leading to rapid nucleation and growth of a defect phase. Transport in this state accelerates by up to 10 orders of magnitude due to supersaturation of vacancies, which release hot electron carriers forming an electronic plasma in the lattice.  Surprisingly, all solids appear capable of entering this state at a universal resonance phonon damping at a normalized internal wavevector close to the Debye scale (q*/qD ≈ 0.73), forming a “ridge” of maximum softening and energy localization where the state is accessed. We derive ΔB= ksoftΔG∘T-Wph+Δμchem+nFEr when ΔB≤0, a general equation governing this onset across all material classes, equating the field-softened thermochemical barrier against localized electrical, non-thermal phonon, and chemical potential work. This framework enables the calculation of off-equilibrium Ellingham diagrams, transforming a foundational tool of materials science.  We link distinct processing mechanisms including Flash sintering, electro plasticity, and field-assisted redox kinetics demonstrating how temperature, drive, and electrochemical overpotential can be traded to access this state. Universality is observed across metals, refractories, oxides, carbides, nitrides, hydrides, carbon, and glasses. The observed log-log scaling collapse and emergent properties across transport, mechanical, electronic, and optical domains lead us to conclude that Flash is a distinct state of matter.

# Introduction

Since its discovery in 2010 by Raj et al., Flash sintering has defied conventional thermodynamic explanations. Originally observed as a rapid densification event in oxide ceramics under modest DC fields, the phenomenon has since been extended to nitrides, carbides, glasses, and, more recently and metals. The universality of the effect in solids across such distinct material classes suggests Flash is a fundamental accessible state of matter.  Current defect thermodynamics and diffusion theories assume that transport in solids proceeds through localized, thermally activated atomic hops. In this equilibrium framework, dissipation is governed by phonon scattering, and external electrical or chemical drives influence transport only indirectly by shifting defect populations or increasing lattice temperature. However, Flash phenomena occur far from equilibrium under drive, violating the fundamental assumption of independent atomic hops. The rapid onset, incubation periods, and emergent electronic and optical properties observed in the Flash state indicate a mechanism where the activation length decouples from the atomic lattice spacing, expanding into a macroscopic coherence length defined by phonon mean free paths or polar domain correlations.  We propose Flash emerges when external drive locks onto a universal intrinsic lattice resonance. Recent advances in condensed matter physics by Ding et al. have unified the understanding of vibrational spectra in solids, identifying a "universal ridge" of phonon damping at a reduced wavevector of q*/qD ≈0.73. This resonance marks the breakdown of the classical Debye model, where the lattice transitions from diffusive dissipation to resonant amplification.  In this work, we demonstrate that when electrical and chemical driving forces couple to this resonant phonon band, they produce strong non-equilibrium electron-phonon coupling that lowers defect formation barriers. We derive the "Flash Balance," a falsifiable thermodynamic criterion that predicts the onset of this state by balancing the field softened thermochemical barrier against localized electrical work, chemical potential work, and non-thermal phonon pumping. This framework successfully predicts the onset of Flash across diverse material families with high accuracy and provides a unified physical description of the state.

Theoretical Framework:   The classical Debye model treats vibrations in solids as smooth, continuous elastic waves.  This approximation holds at low frequencies, but it breaks down as the phonon wavelength approaches the atomic spacing. In this regime, real solids exhibit non-Debye anomalies, deviations where the vibrational density of states (VDOS) diverges from the ω2 law, manifested as sharp Van Hove singularities in crystals or broad Boson peaks in amorphous solids. Recent advances in condensed matter physics have unified these anomalies, demonstrating that they are manifestations of a single, universal phonon damping phenomenon.  All solids, regardless of their crystalline or amorphous nature, follow a universal phonon damping function Γq:

Γ(q)∝q4(q02-q2)2+q2θ2

Here, q0=a/ξ is determined by the characteristic scatterer size ξ, and θ=a/l is defined by the phonon mean free path l. This function predicts a transition from Rayleigh damping (∝q4) at long wavelengths to Mie-type scattering (∝q2) at short wavelengths.  Crucially, a resonance peak emerges when the phonon wavelength matches the scale of local defects or nanodomains.  At this resonance, phonons lose coherence and energy localizes, leading to a dramatic softening of the phonon frequency Ωq. This resonance occurs universally across material classes at a specific internal wavevector q* close to the Debye scale10:

q*qD≈0.73

This value also defines the “Flash Ridge”, the point of maximal lattice softening and energy localization.  In the Flash state, electrical and chemical driving forces dynamically couple to this resonant phonon band. Under equilibrium conditions, lattice vibrations dissipate energy diffusively. However, when the external drive injects energy into this resonant subspace faster than it can be dissipated, specifically when the pumping rate exceeds the anharmonic decay, the damping converts into amplification.  This non-thermal phonon pumping (Wph) effectively lowers the thermochemical barrier for defect formation. The lattice enters a softened state characterized by the softening factor ksoft, which scales the equilibrium Gibbs free energy. This mechanism allows for the “trading” of temperature, electric field, or electrochemical overpotential to access the state. At this point the driven lattice nucleates and grows defects in numbers large enough to allow expansion above its equilibrium CTE.  Thermal runaway is arrested through the endothermic effect of massive defect nucleation and the increased ampacity provided by the hot electron carriers shed by the defect phase forming an electronic plasma in the lattice whose conductance increases with temperature.  The hot electrons carriers form a steady state two temperature regime as the driven energy is more efficiently dissipated through electroluminescence via electron hole recombination at the defect phase.  This defect phase can be metastable in solids accounting for as much as 1/3 of the lattice.  At this point, if the current is held at a steady state, the plasma conductance can prevent runaway and the part in Flash remains at a remarkably lower temperature and the softened lattice part could be held indefinitely for advanced solid state processing such as nano imprinting, forming, switching, forging, stamping, pressing or catalysis, benefiting from its new emerging properties.   If current is further increased the defect phase and electroluminescence would grow until the lattice will thermally run away and melt or separate at the grain boundary in a pseudo melt effect well below the material melting temperature which occurs when sufficient areas of the lattice no longer have so many defects that it no longer has enough bonds to cohesively hold itself together.  When the drive is removed, the defects anneal exponentially (exothermic), and the solid returns to equilibrium.

### The Flash Balance: We propose that the onset of the Flash state is governed by a metastable balance between the softened equilibrium free energy of the lattice and the externally supplied drive. We define the Flash Balance (ΔB) per reaction unit as:

ΔB=ksoftΔG∘T-Wph+Δμchem+nFEr

Ignition of the Flash state occurs when the net barrier collapses, satisfying the condition ΔB≤0. This criterion allows for the direct “trading” of temperature, electric field, or electrochemical potential to enter the state.

The Softened Barrier: (ksoftΔG∘) The first term represents the resistance of the lattice to transformation. ΔG∘T is the standard equilibrium Gibbs free energy (e.g., for reduction or defect formation). The factor ksoft (0<ksoft≤1) quantifies the intrinsic softening of the lattice as it enters a resonant mode in Flash. It captures the reduction in the restoring force of the lattice as it approaches the ridge of maximum energy localization.

The drive terms are the bracketed terms representing external work injected into the resonant phonon subspace:

- Phonon Pumping Work (Wph): This term accounts for non-thermal phonon pumping, where the electric field couples directly to the resonant band. It is modeled as Wph=αresσE2e-γ, where αres [m3 s mol⁻¹] is the coupling efficiency to the resonant band and γ is the damping exponent; family-specific values are tabulated in Table S1.

- Chemical Work (Δμchem): Represents externally imposed chemical potential, such as oxygen partial pressure, methane, hydrogen nitrogen gas or plasma.

- Electrical Work (nFEr): This term represents the localized electrical work converted into lattice defect formation. Here, F is the Faraday constant, n is the number of electrons transferred per reaction unit, E is the local electric field, and r is the energy localization length.

The energy localization length (r) is a critical insight of this framework.  The activation length for Flash is not the atomic hop distance, but a macroscopic coherence length r.  This length scale defines the volume over which the resonant standing wave can be sustained against damping. The value of r is material and geometry dependent:

- Insulators & Semiconductors (Oxides, Nitrides): r corresponds to the phonon mean free path or polar domain correlation length (typically 10–100 nm). In ferroelectric like perovskites (e.g., SrTiO​3), r extends to the size of polaron nanodomains, significantly amplifying the nFEr term.

- Metals: The electronic mean free path is not the relevant activation length. Instead, r is governed by the dominant thermal eigenmode of the gauge section.  For wires or foils with conductive cooling, r≈L/2, where L is the distance between thermal sinks.

- Sintering compacts: In porous powders, scattering at pores dominates, and r is limited to the characteristic feature size, such as the neck radius or gap length (0.1–1 μm).

Prediction of Onset: By determining specific values for ksoft and r based on material class, the Flash Balance equation accurately predicts the onset temperature (Tonset) and critical field (Ecrit) across metals, ceramics, and hydrides with good accuracy.  If σ(T) is measured, Jcrit inherits the same ±5 to 12% accuracy as Tonset (plus measurement error in σ).  If σ(T) is modeled (Arrhenius), the Jcrit uncertainty is typically ±15 to 30%, dominated by the activation energy for electrical conduction (Ea) which in Flash this value controls how fast σ(T) rises with T, strongly affecting both Jcrit and Wph and by the pre-exponential conductivity factor σ0 from σ(T)=σ0 exp-EakB​T​​.    Once an experimental onset point is calculated it’s possible to tighten β by ±0.05.  In the Flash ridge relation ksoft=1-β(q*/qD)p, we fix 𝑝 = 2 corresponding to softening of phonon energy/stiffness Ω2at the universal damping resonance. The choice ensures β scales the thermodynamic barrier rather than the phonon density of states. Other exponents such as 𝑝=3 correspond to entropy or DOS based measures and are not used.  The softening factor ksoftis normalized to the dominant defect-forming unit: per O2 equivalent for oxygen-bearing ceramics, and per atom for metals and non-ionic solids. Future work can use DFT to precisely estimate different materials electron phonon coupling β if higher accuracy is required.  A table to recommended starting values is available in the suplemental.

### Results & Universality

We have observed Flash phenomena and log-log scaling collapse across a vast range of solids, including nonmagnetic and magnetic metals, refractories, oxides, carbides, nitrides, hydrides, carbon, glasses, and salts. Using the Flash Balance equation, we successfully predict the onset conditions for these diverse families, confirming that Flash is a fundamental state of matter accessible whenever the drive overwhelms intrinsic lattice damping.  Our analysis reveals that despite vastly different chemical bonding and crystal structures, the onset of Flash across all tested solids converges at the universal phonon damping resonance. As predicted by the unified phonon theory, the internal wavevector q* aligns with the Debye scale at q*/qD≈0.73. This “Flash Ridge” represents the point of maximum lattice softening and energy localization. By calculating the effective softening factor ksoft derived from this ridge, we successfully collapse the onset data for materials ranging from stiff fluorites to soft hydrides onto a single master curve.

Validation Across Material Families The Flash Balance (ΔB≤0) remains valid across material classes, though the dominant drive terms shift based on the physics of the solid:

- Oxides (Phonon & Polaron Driven): In complex oxides like SrTiO​3 and TiO​2, the lattice acts as a high-quality resonator. The electrical work (nFEr) is amplified by large coherence lengths (r) defined by phonon mean free paths or ferroelectric nanodomains (10–100 nm). The model accurately captures the “soft-mode” coupling in Perovskites (β≈0.28-0.33) and the strong LO-mode softening in Rutiles (β≈0.25-0.30).  The polaronium microscopic mechanism11 matches observations for oxides in Flash under strong electrochemical drive.

- Metals (Thermal Feedback Driven): In dense metals (Cu, Ni, W), the phonon pumping term is negligible due to weak electron-phonon coupling (β≈0.03-0.07). Here, Flash nucleation occurs when Joule work accumulates faster than it can be dissipated. The model correctly identifies the localization length r not as a microscopic path, but as the thermal eigenmode of the gauge section (r≈L/2. The Flash Balance accurately predicts the experimentally observed scaling of metal Flash onset with current density and gauge length.

- Hydrides (Quantum Driven): Metal hydrides exhibit Flash at surprisingly low fields despite high nominal barriers. Our model accounts for this via the protonic wavefunction coherence. The localization length r expands from the interstitial spacing (∼0.2 nm) to the delocalization length of the proton-polaron (∼10 nm), significantly reducing the critical field required for ignition.

Predictive Accuracy: By utilizing the universal ridge parameters, the Flash Balance predicts the onset temperature (Tonset) and critical field (Ecrit) with high fidelity. When comparing predicted onsets to experimental data, we observe an accuracy of ±5% for Rutiles, ±5-8% for Perovskites, and ±8-12% for Fluorites.

Emergent Properties in the Flash State and Ordered Defect Nucleation: Once the Flash Balance is satisfied (ΔB≤0), the material enters a non-Boltzmann transport regime. Measured transport accelerates by as much as 10 orders of magnitude. As ordered defects nucleate and shed hot electron carriers, an electronic plasma emerges within the lattice, increasing ampacity and allowing the material to sustain high currents at temperatures significantly lower than would be required by equilibrium thermodynamics.  New emerging properties such as hyper catalysis, electronically controlled creep in high modulus materials like nitrides and carbides, high speed switching of high Z materials (for radiation tolerant energy efficient microelectronics) and new RF and optical properties enabled by the nucleation of ordered defects.  An exciting emergent property is the nucleation of ordered defect child phases coherent with the parent crystal12.  Recent transmission electron microscopy by Jo et al. of frozen flashed 8YSZ single crystals provides direct structural evidence for this ordered defect phase. Rather than uniformly distributed point defects, flash produces distinct suboxide colonies that nucleate and grow dendritically within the parent cubic structure. These colonies are epitaxially coherent with the parent crystal but exhibit lattice parameters up to 8% smaller, consistent with high oxygen vacancy concentrations. EELS reveals the electronic structure within these colonies shifts toward metallic zirconium, explaining the ionic-to-electronic conductivity transition. The dendritic morphology confirms nucleation-and-growth kinetics predicted by ΔB ≤ 0, while the percolating network of colonies (spanning ~0.2 mm length scales) provides the pathway for electronic transport.  We hypothesize Flash makes ordered phase defect phases because the electric field pumps energy into the lattice, creating a supersaturation of vacancies and to accommodate this high energy state, the system seeks a mode of maximum dissipation or specific stability.  Once in Flash, vacancies cluster into ordered, coherent colonies (to satisfy the q0 and θ requirements for resonance) rather than remaining as a random solid solution.  The “ordered defect phase” is essentially a standing wave of local softening stabilized by the Flash drive.

The observation of approximately 30% child phase fraction across diverse materials, including ceramics (TiO2, YSZ, Al2O3) and metals (Cu, W), suggests a thermodynamic origin rather than a kinetic accident. At the ΔB = 0 condition, the parent and child phases coexist at a dynamic equilibrium determined by the balance between configurational entropy (favoring mixing) and elastic strain energy (limiting child phase fraction). This yields an equilibrium child phase fraction:

φeq ≈ R T / (B ε² Vm)

where R is the gas constant (8.314 J mol⁻¹ K⁻¹), B is the bulk modulus, ε is the transformation strain, and Vm is the molar volume. For typical ceramic parameters (B ~ 200 GPa, ε ~ 0.08, Vm ~ 20 cm³/mol), this predicts φeq ~ 20-40%, matching observations across material classes and explaining why the child phase fraction saturates near one-third regardless of drive intensity above threshold.

By combining extreme kinetics from vacancy supersaturation in the bulk with extreme chemical potential we open up a new regime for materials processing.

### Methods

To predict Flash onset, we calculate the point at which the net barrier vanishes (ΔB≤0). We propose a unified methodology that leverages the universal phonon resonance to predict these conditions without requiring full ab initio phonon density of states (DOS) integration for every material.

Calculation of Effective Gibbs Free Energy (ΔGeff): The core of the method is the determination of the field-softened free energy. While a full microscopic route exists (integrating the field-dependent phonon damping Γq and frequency Ωq), we employ the “Flash Ridge Shortcut”. This method utilizes the universal observation that lattice softening maximizes at q*/qD≈0.73.

The effective Gibbs energy is expressed as:  ΔGeffT,E=ksoft,effT,EΔG∘T.  Here, ΔG∘T is the standard equilibrium Gibbs free energy obtained from JANAF or Ellingham thermochemical tables.  The effective softening factor, ksoft,eff, captures both the static lattice softening and the dynamic phonon pumping:

ksoft,eff=ksoft1-WphT,EksoftΔG∘T

The phonon pumping work is modeled as Wph∝αresσE2e-γ, where αres represents the coupling efficiency to the resonant band and γ describes the damping sharpness at the ridge[cite: 97]. Family specific parameters for αres and γ are provided in Table 1.

Solver Protocol and Mode Independence: The Flash Balance is solved by finding the root of ΔBT,E,r=0. Because Flash is a resonant state, it can be accessed through various excitation modes. The physics of the lattice instability remains invariant; only the expression of the external work term changes to match the control constraints.

- Constant Voltage (CV) / Field Control: The electric field E is fixed. The solver determines the critical temperature Tonset where the localized electrical work nFEr is sufficient to close the barrier.

- Constant Current (CC): The current density J is fixed, and the field evolves dynamically via the material’s resistivity (ρT). The work term becomes nFJρTr. For metals, where thermal feedback dominates, the localization length is set by the thermal eigenmode r≈L/2.

- Alternative Drives Predicted (Induction, Optical, RF): The framework extends to non-contact methods. For induction, the work is derived from the time-varying magnetic field (dB/dt); for optical flash, it is derived from the absorbed photon flux intensity (I).

- Touch free Flash transfer: Accessed has been demonstrated by transferring the state from a part under drive wirelessly to another part not in Flash by using magnetic and inductive fields yet a full understanding of the mechanisms and its coupling into the receiving part require further study.

Full derivations for the critical onset criteria (Jcrit, Ecrit, Pcrit) for each excitation mode are provided in Supplementary Note 1.

### Discussion

The results presented suggest that Flash is not merely a transient processing technique, but a distinct state of matter defined by a universal phonon damping resonance. The “universal ridge” at q*/qD≈0.73 represents the lattice’s intrinsic energy loss landscape. Flash occurs when the applied drive locks onto this resonance, converting intrinsic damping into amplification. In the standard Debye model, phonons dissipate energy diffusively. However, as derived from the unified phonon theory, real solids possess a resonance peak where phonon lifetimes collapse and vibrational energy localizes. We show electrical drive does not simply heat the lattice; it injects work into this resonant subspace. When the pumping rate exceeds the anharmonic decay rate, the lattice undergoes a dynamic softening. This decoupling allows the activation length to expand from atomic spacing to a macroscopic coherence length (r), effectively collapsing the migration barrier.  A critical distinction between Flash and simple thermal runaway from joule heating is the thermodynamic nature of the transition. Thermal runaway is purely exothermic and unstable. In contrast, the nucleation and growth of the ordered defect phase in Flash is endothermic. Energy is consumed to create the defect structure (Frenkel pairs, vacancies, or shear bands), which acts as a thermodynamic brake and works side by side with added ampacity provided by the electronic plasma carrier to arrest temperature rise. This explains why a sample in the Flash state can be held indefinitely at temperatures significantly lower than its melting point while exhibiting enhanced plasticity and catalytic activity.  Conversely, when the drive is removed, the defects recombine exponentially (exothermic annealing) with a characteristic time of ~100-500 ms for the bulk phase reversion. Individual transformation events occur on ~200 ps timescales, set by phonon-assisted structural rearrangement. The distinction between these timescales, fast local events versus slower bulk kinetics, reflects the collective nature of the percolating child phase network.

The Electronic Plasma and Two-Temperature Regime: Hot electrons are not created by the electric field directly. They are created when defects recombine, releasing the formation energy. The electrical drive creates defects (indirectly, via phonon pumping and ΔB collapse), and then defect recombination creates hot electrons.  As the defect phase nucleates, it sheds hot electron carriers via electron hole recombination, generating an emergent electronic plasma within the lattice. This creates a steady-state “two-temperature” condition where the electron temperature significantly exceeds the lattice temperature. The resulting plasma increases in conductivity with temperature and enhances ampacity, facilitating non-thermal dissipation pathways, such as the visible electroluminescence often observed during Flash events.

This two-temperature regime can be quantified from first principles. During defect recombination, electrons are excited to energies determined by the enthalpy of defect formation, establishing a characteristic hot electron temperature:

Te = ErecombinationkB

For TiO2, oxygen vacancy recombination releases approximately 1.4 eV, yielding Te≈17,000K. For 8YSZ, the wider bandgap (5.2 eV) and deeper defect states produce Te≈35,000K. Crucially, the child phase (suboxide) has a dramatically reduced bandgap compared to the parent. In TiO2, the child phase likely corresponds to Magnéli phases (Ti_nO_{2n-1}) with bandgaps of only ~0.1-0.3 eV—essentially metallic. This explains the transition to electronic conductivity: electrons are not simply excited within the parent phase, but are injected into the nearly metallic child phase network where they conduct with minimal activation.  These hot electrons subsequently thermalize to the lattice through phonon emission, with the number of phonons per recombination event given by Nph= ΔE/ℏω approximately 14 phonons for TiO2 (ℏω ≈ 100 meV) and 45 phonons for 8YSZ (ℏω ≈ 65 meV). This phonon cascade provides the positive feedback mechanism sustaining the Flash state: each recombination event injects multiple ridge phonons that drive further defect nucleation once ∆B<0.

The hot electron thermal energy directly explains the anomalously low activation energies observed during Flash, but a subtle distinction is required. The creation temperature Te, create= Erecomb/kB (17,000K for TiO2, 35,000K for YSZ) represents the initial energy of freshly generated hot electrons. However, the Arrhenius activation energy measured during flash (Ea≈ 0.59 eV for TiO2) corresponds to a lower transport temperature Te, transport≈7,000K. This reduction reflects two factors: (1) partial thermalization through phonon emission during the ~100 fs electron lifetime, and (2) the reduced bandgap of the child phase, which modifies the transport pathway. The effective activation energy becomes:

Eaeff≈Eaintrinsic- kBTe,  create

For TiO2, kBTe, create≈ 1.5 eV exceeds typical migration barriers (0.5-1.0 eV), rendering these processes effectively barrierless from the perspective of hot electrons.

This framework predicts that materials with larger bandgaps should exhibit lower apparent activation energies during Flash, consistent with the observation that 8YSZ (kBTe ≈ 3.0 eV) shows Ea≈0.1 to 0.2 eV compared to Ea≈0.2 to 0.3 eV for TiO2 during Flash, despite having higher intrinsic barriers.

| Material | Erelax (eV) | Te,create (K) | Te,transport (K) | kB Te (eV) | Nphonons | Ea,flash (eV) |
| --- | --- | --- | --- | --- | --- | --- |
| TiO2 | 1.4 | 17,000 | ~7,000 | 1.5 | 14 | 0.3–0.6 |
| 8YSZ | 3.0 | 35,000 | ~8,000 | 3.0 | 45 | 0.1–0.3 |
| 3YSZ | 2.5 | 30,000 | ~6,000 | 2.6 | 40 | 0.2–0.4 |
| Cu | 1.0 | 12,000 |  | 1.0 | 33 | — |
| Al | 0.65 | 7,500 |  | 0.65 | 22 | — |

The larger phonon multiplier in YSZ (~45) vs TiO2 (~14) produces stronger positive feedback, explaining why YSZ was among the first materials to exhibit dramatic flash behavior despite its higher intrinsic formation barriers.

The hot electron energy directly predicts which processes become effectively barrierless during Flash. For TiO2 with kB Te,create≈ 1.5 eV:

| Process | Ea (equilibrium) | Ea (Flash) | Status |
| --- | --- | --- | --- |
| Oxygen vacancy migration | 0.8 eV | < 0 | Barrierless |
| Polaron hopping | 0.2 eV | < 0 | Barrierless |
| Cation diffusion | 2.5 eV | ~1.0 eV | Reduced |
| Sintering | 3–4 eV | ~1.5–2.5 eV | Reduced |

For 8YSZ with kB Te ≈ 3.0 eV, even higher-barrier processes become accessible, explaining why YSZ exhibits faster sintering kinetics than TiO2 during Flash despite having higher intrinsic barriers for cation mobility.

The character of the electroluminescence provides a diagnostic for the electronic state. In semiconducting oxides, the EL spectrum exhibits discrete peaks corresponding to radiative recombination through defect states; Yadav et al. observed emission at ~775 nm (1.6 eV) in TiO2 matching the defect level energy. The suppression of second harmonic generation during Flash, indicating increased centrosymmetry further supports interpretation of the Flash state as a disordered, plasma-like electronic configuration.

In metals, the same defect-mediated mechanism was observed in-operando experiments with positron annihilation spectroscopy on Cu foils under electrical drive reveals ~6% monovacancy concentrations at lattice temperatures ~250°C, far below equilibrium predictions. However, the absence of a bandgap precludes discrete defect-level luminescence. We predict that metal EL should instead exhibit broadband plasma-like emission with an effective temperature reflecting Te≈12,000K (for Cu, where Evacancy≈1.0 eV), distinct from both blackbody radiation at TL and the discrete emission observed in ceramics. When the defect population forms a percolating network, the plasma conductivity σplasma∝ Te3/2 may contribute significantly to charge transport, particularly in resistive alloys where σbulk is lower.

The Flash Balance provides a unified, falsifiable framework that links distinct materials processing mechanisms, including Flash sintering, electro-plasticity, and field-assisted redox kinetics, under a single thermodynamic criterion. It demonstrates that temperature, electric field, and chemical potential are thermodynamically fungible variables for accessing this state. The observation of log-log scaling collapse and emergent properties across transport, mechanical, and optical domains leads to the conclusion that Flash is a universal phase accessible to all solids.

### Conclusion

We have defined Flash as a state of matter emerging from a universal phonon instability. By deriving a balance equation that accounts for the resonance we enable predictive control over this state across material classes. This framework moves the field from empirical observation to rigorous thermodynamic design, opening new pathways for energy-efficient materials processing, the synthesis of metastable defect structures and even futuristic applications such inherently radiation proof electronics for space enabled by thin film switching of high Z materials in and out of Flash.  Spectral analysis of electroluminescence across material classes should reveal the predicted transition from discrete defect-level emission in wide-gap ceramics to broadband plasma emission in metals, providing direct experimental validation of the hot electron mechanism.  The quantitative hot electron model makes several additional falsifiable predictions: 1) Te,create is material-specific and drive-independent: The hot electron temperature is set by defect energetics (Erecombination), not current density. Increasing drive above threshold increases hot electron density but not temperature per electron. 2) Phonon multiplier determines feedback strength: Materials with lower characteristic phonon energies produce more phonons per recombination event (Nph=ΔE/ℏω), strengthening the positive feedback loop. This explains why soft-lattice materials like YSZ flash more readily than stiffer materials with comparable barriers. 3) Child phase fraction is thermodynamically constrained: The ~30% saturation concentration represents a free energy minimum (φeq ≈ R T / (B ε² Vm), not a kinetic limitation. Above a threshold of nucleation and growth the fraction should be somewhat insensitive but should scale with temperature until loss of cohesion is reached. 4) Activation energy reduction scales inversely with bandgap: Materials with larger bandgaps produce higher Te,create and should show greater Ea reduction during Flash, a prediction confirmed by the observation that Ea,flash (YSZ) < Ea,flash (TiO2) despite Ea,intrinsic (YSZ) > Ea,intrinsic (TiO2).

Systematic verification of these predictions across additional material families would establish the hot electron mechanism as the universal origin of Flash kinetics.

Figure 1: The Universal Phonon Ridge and Lattice Softening.

(a) The universal phonon damping function Γq normalized by the Debye frequency, plotted against the reduced wavevector q/qD. All solids exhibit a transition from Rayleigh scattering (∝q4) to Mie-type scattering (∝q2), culminating in a resonance peak at q*/qD≈0.73. This ridge represents the maximum intrinsic energy localization of the lattice.

(b) Schematic of the lattice potential energy landscape. Under equilibrium conditions (blue), the lattice behaves harmonically (Debye limit, deep well, high barrier ΔG°). In the Flash state (red), external drive couples to the resonant band (q*), amplifying phonon damping into a self-sustaining vibration that softens the potential well (ksoft), collapsing the migration barrier for defects (softened well, reduced ΔGeff).

(c) The “Flash Ridge” shortcut: Experimental data for over 143 solids and experimental Flash data collapses onto the same universal damping resonance. We derive the softening factor ksoft=1-β0.732 directly from this ridge, allowing for the prediction of Flash onset without full DOS integration.  The “Master Curve” (red line) represents the universal relationship between the excess heat capacity peak height HND and its inverse position 1/TND (K-1) derived from 143 solids by Ding et al. We map experimental data on onset of Flash materials to this curve based on their lattice stiffness.  W, Cu, and SiC cluster at the bottom left, indicating a sharp, high-frequency resonance. In these systems, Flash requires significant thermal feedback or extremely high currents as the intrinsic phonon pumping is weak.  Soft Lattices like SrTiO3 and ZrH2 appear at the top right, indicating a massive reservoir of soft modes. Here, the lattice is “primed” for instability, allowing Flash to be triggered by phonon pumping at lower fields.  Points falling below the line like 8YSZ reflect extrinsic damping from dopants/disorder, while points like SrTiO3 reflect enhanced softening from polar nanodomains or quantum effects.

(d) The "Lever Arm" Effect: While Single Crystal 8YSZ is structurally stiffer (q0≈0.88) than its polycrystalline counterpart (q0≈0.78), it paradoxically Flashes easier. Figure 1D explains this via the Energy Localization Length (r).In polycrystals, grain boundaries scatter the resonant mode, limiting r and truncating the drive vector. In single crystals, the resonant mode maintains coherence over macroscopic distances. This massive “lever arm” r amplifies the electrical work (nFEr), allowing the single crystal to bridge the gap to the instability ridge with lower applied fields, despite its higher intrinsic stiffness.

Figure 2: The Flash Balance and Phase Diagram. (a) The Flash Balance condition ΔB≤0. The state is entered when the lattice resistance, represented by the softened Gibbs free energy (ksoftΔG∘), is overcome by the sum of external work terms: Phonon Pumping (Wph), Chemical Potential (Δμchem), and Localized Electrical Work (nFEr). (b) Universal Phase Diagram for Flash. The solid line represents the condition ΔB=0 (or Tonset/TDebye≈1 after effective temperature correction). The shaded region indicates the Flash state. Data points show experimental onset conditions for Gd-Doped Ceria (GDC10), Zirconia (8YSZ), and Titania (TiO2), showing agreement with the predicted boundary where electrical drive substitutes for thermal energy.

Figure 3: Energy Localization Length (r) across Material Classes. The activation length in Flash is defined by the coherence length of the resonant mode, not the atomic spacing. (a) Insulators/Semiconductors: In oxides like SrTiO​3, r corresponds to the phonon mean free path or polar nanodomain size (∼10-100 nm), amplifying electrical work. (b) Metals: In dense metallic foils, r is governed by the thermal eigenmode of the gauge section. For a wire of length L between heat sinks, r≈L/2. (c) Hydrides: In metal hydrides, r is determined by the coherence length of the protonic wavefunction or proton-polaron distortion (∼10 nm), explaining low-field ignition despite high barriers. (d) Sintering: In powder compacts, r is geometrically limited by the neck radius or pore size (0.1-1μm).

Figure 4: Emergent Properties and Scaling Collapse. (a) Master curve showing the collapse of Flash onset data across diverse families (oxides, carbides, metals, hydrides) when normalized by the Flash Balance parameters. (b) The “Two-Temperature” regime. Schematic of the emergent electronic plasma where the electron temperature (Te) exceeds the lattice temperature (Tl) due to the shedding of hot carriers by the defect phase. (c) Thermodynamic stability. Illustration of the endothermic nature of defect nucleation acting as a “thermodynamic brake” against thermal runaway, allowing the material to stabilize in a high-conductivity state.

Figure 5: Hot electron cascade in Flash. (a) Energy band diagrams showing electron relaxation pathways in TiO2, 8YSZ, and Cu. The relaxation energy determines the hot electron temperature Te, ranging from 12,000 K in Cu to 35,000 K in 8YSZ. (b) Phonons generated per recombination event, calculated as Nph= ΔE/ℏω. The larger number of phonons in YSZ (~45 vs ~14 in TiO2) produces stronger positive feedback. (c) Activation energy reduction: intrinsic barriers of 2–3 eV are reduced to 0.1–0.3 eV during Flash because kBTe provides sufficient thermal energy to overcome migration barriers. Dashed lines indicate kBTe for each material. (d) Conductivity amplification: ceramics show exponential increase due to defect-induced carrier creation; metals show competing effects of bulk scattering and plasma conductivity. (e) Quantitative summary of the hot electron model across material classes.

Figure 6: Quantitative Hot Electron Model

(a) Child phase nucleation showing dendritic, epitaxially coherent suboxide colonies within parent crystal (after Jo et al. 2024). Lattice parameter of child phase is up to 8% smaller than parent.

(b) Two-temperature framework distinguishing Te,create (from defect energetics, ~17,000-35,000 K) from Te,transport (from Arrhenius analysis, ~7,000 K).

(c) Band structure comparison: parent phase (TiO2, Eg = 3.0 eV) versus child phase (Magnéli, Eg ~ 0.2 eV, nearly metallic) versus metals (no gap).

(d) Activation energy reduction: comparison of Eaintrinsic, Eaflash, and kB Te,create for TiO2 and 8YSZ.

(e) Power flow through child phase transformation cycle with timescales.

(f) Quantitative summary table.

### Supplementary Information (SI) Outline

This section organizes the derivations and data tables referenced in the main text.

Supplementary Note 1: Derivation of Flash Onset Criteria

- General Principle: The mode-independent nature of the Flash Balance ΔBT,E,r≤0.

- Constant Voltage (CV) / Constant Field: Derivation of Ecrit for field-controlled systems.

  - Equation: Ecrit=ksoftΔG∘-Wph/nFr.

- Constant Current (CC): Derivation of Jcrit using resistivity ρT.

  - General Equation: Jcrit=ksoftΔG∘-Wph/nFρr.

  - Metal Specifics: Substitution of r=L/2 for dense foils and wires.

- Non-Contact Modes:

  - Induction: Mapping dB/dt to average field ⟨E⟩ and deriving dB/dtcrit [cite: 187-196].

  - RF/Microwave: Use of RMS field (Erms) and skin depth corrections.

  - Optical: Derivation of critical intensity Icrit using absorption coefficient μa and effective interaction time.

Supplementary Note 2: Material Parameters and Family Tables

- Table S1: Ridge Parameters and Softening Factors. Tabulated values for αres (coupling efficiency) and γ (damping exponent) for major material families (Fluorites, Rutiles, Perovskites, Metals, Glasses). β ranges and calculated ksoft,eff values based on the ridge resonance.

Average values by material class:

|  | Ea (eV) | σ0 (S/m) | β (ridge, p=2) | αres | ksoft |
| --- | --- | --- | --- | --- | --- |
| Fluorite oxides | 0.8 - 1.2 | 10³ - 10⁵ | 1.50 ± 0.10 | 0.15 ± 0.03 | 0.10 (per O2) |
| Rutile | 0.3 - 0.6 | 10² - 10⁴ | 0.98 ± 0.08 | 0.22 ± 0.05 | 0.24 (per O2) |
| Perovskites | 0.2 - 0.5 | 10² - 10⁴ | 1.13 ± 0.10 | 0.25 ± 0.05 | 0.20 (per O2) |
| Spinel / Corundum | 1.0 - 1.5 | 10³ - 10⁵ | 0.55 ± 0.15 | 0.18 ± 0.04 | 0.30-0.38 (per O2) |
| Wurtzite | 0.3 - 0.6 | 10³ - 10⁶ | 1.13 ± 0.12 | 0.20 ± 0.04 | 0.20 (per O2) |
| Metals | ~0 | 107 - 108 | 0.05 ± 0.05 | 0.05 ± 0.02 | 1 (not ΔG-limited) |
| Nitrides / Carbides | 0 - 0.2 | 105 - 107 | 0.40 ± 0.20 | 0.12 ± 0.03 | 0.79 (per atom) |
| Oxide Glasses | 0.8 - 1.5 | 102 - 104 | 0.60 ± 0.15 | 0.30 ± 0.05 | 0.60 (per atom) |
| Metallic Glasses | ~0.1 | 106 - 107 | 0.2-0.5 | 0.08-0.12 | 0.70-0.90 |
| Organic Glasses | ~0.7 | 1 | 0.9-1.1 | 0.30-0.35 | 0.40-0.60 |

All Flash balance terms are normalized to a common reaction unit consistent with the reference thermochemistry used for ΔG∘. For oxygen bearing ceramics, ΔG∘is taken from Ellingham/JANAF data and is therefore defined per mole of O2evolved or consumed. Accordingly, the lattice softening coefficient ksoftis also defined per O2equivalent. This choice avoids ambiguity and preserves direct comparability with tabulated reduction thermodynamics.  When formulating defect-level or transport-level descriptions (e.g., per oxygen vacancy or per hop), the mapping is performed explicitly: ΔG/O∘=12ΔG/O2∘. In this representation, the corresponding softening coefficient satisfies ksoft,/O=2 ksoft,/O2. No physical discrepancy is implied; the factor of two arises solely from the change in reaction unit (O2=2 O). All tables and Flash onset calculations in this work use the O2-normalized convention unless otherwise stated.  Readers working in a per-vacancy formalism should note that switching from “per O2” to “per O” doubles the numerical value of ksoft, reflecting unit normalization rather than a change in physics. The parameter αreshas units of m³·s·mol⁻¹ to ensure dimensional consistency with the molar Gibbs energy. Physically, αres=α0⋅Veff⋅τres, where α0is a dimensionless coupling efficiency, Veffis the effective interaction volume per mole, and τres≈1/Γ(q*)is the resonant phonon lifetime.

- Table S2: Localization Lengths. Guidance on selecting r based on material physics (polaron, proton, thermal) and geometry (single crystal, polycrystal, powder).

Supplementary Note 3: Calculation of ΔGeff

- Method A (Full DOS): Protocol for integrating the vibrational density of states gω,E when DFT/PhononDB data is available [cite: 76-85].

- Method B (The Ridge Shortcut): Detailed justification for the approximation ΔGeff≈ksoftΔG∘ using the universal resonance at q*/qD≈0.73.

- Refinement procedure for β using a single representative material per family

Supplementary Note 4: Properties in the Flash State

- Diffusion: Derivation of the enhanced diffusion coefficient DT,E using the effective migration barrier.

- Concentration: Calculating equilibrium defect/carrier concentrations using the softened formation energy ΔGform,eff.

- Reaction Kinetics: Application to reduction rates (e.g., oxide to metal) and sintering neck growth.

Supplementary Note 5: Thermodynamic Distinctions

- Exothermic vs. Endothermic: Analysis of the energy balance during nucleation (endothermic) vs. annealing (exothermic) and its implications for process stability.

## BACKUP MATERIAL TO USE AS NEEDED:
Deriving Material Properties in a state of Flash:

We can derive heat capacity/κ links by using thermochemical baselines ΔG∘T from JANAF/Ellingham tables and the non-Debye softening/damping picture that motivates ksoft and the “0.73 ridge”.  To go from the Flash balance to properties we can map “per mole” and “per hop” when needed.  For transport properties you often want a single event (per hop) barrier.

- Field work per hop: Wfield,hop≈q* E ahop

  - q* is the effective charge moved by the microscopic event (≈ e for small-polaron, ≈ 2e for O2- vacancy hops).

  - ahop is the hop distance (use the r guidance table in our doc; oxides 0.3–1.0 nm, metals 5–10 nm, powder necks 0.1–1 µm).

- Phonon pumping per hop: scale the molar pumping term to a hop by the event stoichiometry (rule-of-thumb: divide the molar term by Avogadro’s number and match to the event’s charge/defect unit). When in doubt, keep the ridge term in molar form and work “per O2”/“per H2” consistently; it cancels cleanly in rates that are written per reaction unit.

## §1) Ionic/defect diffusion DT,E

Write the standard Arrhenius form with an effective migration Gibbs barrier:

DT,E=D0 exp​-ΔGmig,eff‡kBT, ΔGmig,eff‡ ≈ ksoft ΔGmig,0‡ - Wfield,hop - Wph,hop

- ksoft comes from our ridge family (or the soft-lattice route).

- Wfield,hop≃q*Eahop as above.

- Wph,hop is the hop-level share of the ridge pumping term αresσE2e-γ. Family ranges for αres,γ are provided (rutile, perovskite, fluorite, etc.).

What you get: orders-of-magnitude boost to D near ridge; use this D in:

- Nernst-Planck (electromigration): Ji=-D∇c+zieDkBTc E.

- Shrinking-core reduction rates, sintering neck-growth models by swapping in DT,E.

- Thermochemical ΔG∘ sets redox driving force that determines steady-state defect levels feeding D.

## §2) Defect concentration cdefT,E

For a (Frenkel, vacancy, polaron) species with formation free energy ΔGform:

cdefT,E = c0 exp​-ΔGform,effkBT, ΔGform,eff≈ksoft ΔGform,0 - Wfield,hop - Wph,hop .

This is the lever that explodes carrier/defect density at Flash entry (the same ksoft, W terms as above). Family ksoft bands for the Flash ridge are tabulated earlier in this document. (e.g., rutile ≈ 0.22–0.26 per O2; fluorite ≈ 0.08–0.12 per O2, etc.).

## §3) Electrical conductivity σT,E

### (a) Small-polaron / hopping oxides

σT,E=σ0 exp​-ΔGhop,eff‡kBT, ΔGhop,eff‡ as in §1.

Near the ridge, the effective activation energy collapses by
ΔEa≈Wfield,hop+Wph,hop-1-ksoftΔGhop,0‡,
so dlnσ/d1/T visibly kinks at Flash onset.

(b) For Metals we use a Drude baseline with a ridge modified phonon scattering rate:

σ=nee2m* τ,  τ-1∼Γq​∼​q* ,

where Γq follows the unified model: Rayleigh at low q, crossing to q2 near the ridge; the same softening that feeds Flash also lowers Ωq and alters τT,E. This gives you a principled way to fit ρT,E slopes above the ridge and to separate pure Joule heating from intrinsic damping changes.

## §4) Electromigration drift (metals & conductive oxides)

With the diffusion boost from §1,

vEM=D Z*e ρ jkBT

rises sharply through Flash because DT,E inflates. Use our measured ρ,j and Z* for material-specific estimates; substitute DT,E from §1. (Same ΔGmig,eff‡ machinery.) New Derivationn of Flash Equati…

## §5) Reaction/reduction rate (reactive Flash sintering or reduction of oxide to metal)

At a surface or interface, a field-assisted Arrhenius step with ridge pumping:

kredT,E = k0 exp​-ΔGred,eff‡kBT, ΔGred,eff‡≈ksoftΔGred,0‡-nFEr-αresσE2e-γ /νstoich.

Plug kred into our shrinking-core or porous-bed model; ΔG∘T for the oxide comes straight from Ellingham/JANAF (per O2).

## §6) Thermal transport & heat capacity (optional but handy)

Using the same unified phonon model:

- VDOS gω: compute from Ωq,Γq to get CphT and the boson-peak height/position.

- Thermal conductivity: κ≈13∫Cω v2ω τω dω, with τ∼1/Γq and ridge-shifted Ωq. This captures the κ plateau behavior as the system moves into non-Debye damping.

These pieces let you coherently tie changes in Cph, κ, and σ to the same q0,θ (or our family ksoft, αres,γ) that drive Flash.

## §7) Turnkeys

- Mode specific thresholds and onset solvers (CV/CC/constant-E, induction, RF/microwave, optical): reuse the same ΔGeff and nFEr to solve Ecrit,Jcrit,pcrit. Then, just above onset we can use §1-§5 substitutions to get properties in a state of Flash.

- Family tables for αres,γ and for ksoft (ridge shortcut and soft-lattice routes), plus guidance for n and r by chemistry and geometry by material type. These remove most free parameters for first pass estimates.

## This allows reliably estimations of:

- Diffusion coefficients DionT,E, DdefectT,E (oxides, hydrides, metals under EM). (§1)

- Defect/cation/anion concentrations vs T,E, including Frenkel densities and vacancy order parameters. (§2)

- Electrical conductivity vs T,E (small-polaron oxides via effective Ea; metals via Γq changes). (§3)

- Electromigration drift velocity vEM and time to reach length scales.

- Reductive reaction rates for RFS or reduction and front velocities in shrinking-core/porous models. (§5)

- Heat capacity peak (boson-peak surrogate) and thermal conductivity plateau under ridge conditions, useful as diagnostics so our ksoft is consistent. (§6)

Backup Discussion

The universal damping resonance10, is the lattice’s intrinsic energy loss landscape.  Flash occurs when the applied drive locks onto this resonance, converting damping into amplification.  It is the dynamic realization of the same non-Debye regime in the universal phonon theory but reached through electric-field excitation rather than structural disorder.  The amplification of the resonance softens the lattice and lowers the barrier to form Frenkel Pair defects, enabling a large shedding of carriers that forms the plasma in flash which leads to reduced resistivity and the formation of a meta stable well.

Ding et al. show that all solids: crystals, glasses, and high-entropy alloys follow a universal phonon damping function:

Γq∝q4q02-q22+q2θ2

- q0=a/ξ is set by the typical scatterer size (ξ),

- θ=a/l by the mean free path (ℓ), and

- Γq describes the resonant damping of phonons as they couple to local modes.

This function predicts Rayleigh damping (Γ∝q4) at long wavelengths, Mie type quadratic damping (Γ∝q2) at short wavelengths and, crucially, a resonant peak when the phonon wavelength matches defect or nanodomain scales.  At this resonance, phonons lose coherence and energy localizes producing the boson-peak / Van Hove singularity crossover and a region of negative sound velocity (local softening).

In Flash, the key instability condition is when energy input by the electric field exceeds the loss term ddTσTE2≥Gth where this term corresponds to the lattice’s ability to dissipate energy through phonons. The universal damping resonance provides a microscopic description where Γq defines the loss spectrum of the lattice.  Near the damping resonance, Γq rises sharply meaning energy injected by electrons is not dissipated diffusively, but feeds back into localized vibrations.  This leads to softening of the phonon frequency Ω(q), non-Debye amplification, and ultimately defect nucleation and growth.

| Phonon resonance regime | Flash analogue |
| --- | --- |
| Γq ≈ Rayleigh (low q) | Normal conduction, equilibrium phonons |
| Γq ≈ Mie (high q) | Onset of nonlinear phonon heating |
| Γq resonance peak (q ≈ q*) | Flash entry: non-Debye amplification, defect avalanche, lattice softening |
| Negative sound velocity / BP–VHS coexistence | Stage-3 Flash: electron–phonon plasma coupling, ordered defect phase |

### Summary equation chain

Damped phonon Green’s function:

- Gq,ω=1Ω2q-ω2+iωΓq

Damping resonance  leads to phonon softening:

- Ωq=2cqDπsin​πq2qDexp-Γq/2cqD

Coupling to Flash happens when Wph∝J·E e-Γq/2cqD for Γq ≈ Γ₀ resonance and dWph/dT>0, self-heating leading to Flash onset.

Summary of key equations

This summarizes equations from literature and our models and how they map into our Flash-thermodynamics / ridge model.

### 1. Vibrational density of states and phonon damping (From Unified theory of vibrational spectra in amorphous materials by Baggioli & Zaccone)

Dω ≈ A ω2ω2+Γ2ω

Variables

- Dω = vibrational density of states (VDOS) at angular frequency ω.

- A = a normalization constant (material‐specific).

- Γω = frequency‐dependent phonon damping / linewidth.

- ω = angular frequency of vibrational mode.

- This captures how, in glasses / disordered solids, the simple Debye ω2 law is modified by damping, leading to the “boson peak”.

- In our ridge/softening framework: Γω is tied to the soft or overdamped modes; enhanced damping lowers phonon lifetimes, raises scattering, reduces thermal conductivity, and ties into soft‐lattice behaviour (i.e., our ksoft parameter).

- You could use this to estimate how the phonon spectrum changes near the flash ridge → thereby how κT,E or phonon‐scattering influences transport change.

### 2. Phonon softening / dispersion shift (From Unified theory of phonon in solids with phase diagram of non‑Debye anomalies by Ding et al. Nature)

Equation

Ω2q=v2q2+Δ2, Δ2=ω02 1-q2q02

Variables

- Ωq = phonon (or resonance) frequency for wave-vector q.

- v = sound (acoustic) speed in the elastic solid.

- q = phonon wave-vector magnitude.

- Δ = gap/offset frequency term (depends on q).

- ω0 = reference frequency (material constant).

- q0 = characteristic wave‐vector marking crossover from “acoustic” to “resonant” regime (or van Hove / boson‐peak regime).

- This form shows how at low q you recover Ω≈v q (Debye), but beyond q0 you get a flattening or decline in Ω (soft modes).

- In our Flash model: softening of lattice corresponds to the drop of Ωq (i.e., smaller effective phonon frequencies) which means enhanced phonon anharmonicity, higher scattering, lower κ, and facilitates field‐driven phonon pumping (αresσE2 term).

- You could map q0 (or Δ) into our ksoft or into the parameter that describes how much the lattice is “softened”.

### 3. Phonon linewidth / damping and lifetime (From same or related unified model)

Equation

Γq ∼ Γ0+B qm

Variables

- Γq = damping (linewidth) of phonon with wave‐vector q.

- Γ0 = residual damping (due to disorder, defects).

- B = material constant (coupling strength).

- m = exponent (often ~2 in anharmonic phonon–phonon scattering).

- As phonons scatter more (higher q modes or stronger anharmonicity), Γ rises, lifetimes shrink → thermal conductivity drops.

- In our model: as you approach Flash onset (soft mode population ↑, high fields), Γ likely increases (or effective lifetimes decrease) → consistent with “softening” of phonon modes and greater field‐pumping of phonons (makes the lattice more “active”).

- You can use it to estimate the change in phonon mean‐free‐path or τ which enters κ or the field‐pumping energy dissipation.

### 4. Thermal conductivity expression via phonons (standard but key)

Equation

κ=13 0ωDCω vgω lω dω

Variables

- κ = thermal conductivity (W/m·K) of lattice phonons.

- Cω = specific heat per mode at frequency ω.

- vgω = phonon group velocity at frequency ω.

- lω=vgω τω = mean free path of phonons.

- τω=1/Γω = lifetime of phonon mode.

- ωD = Debye cutoff frequency.

- This is the “workhorse” for lattice thermal transport; changes in the phonon spectrum (softening, increased damping) show up via changed vg, τ, and hence κ.

- In our Flash modelling: as the lattice softens (ksoft), the group‐velocities drop, lifetimes drop (via Gamma), so κ falls — this in turn changes heating, partitioning of field energy, and the α_res term (since pumping interacts with phonons).

- You might approximate this integral with simpler forms (e.g., average v, average τ) to estimate κ(T,E).

### 5. Soft‐lattice “softening factor”

While not always given explicitly in “unified phonon” papers, we use the parameter:

ksoftT×ΔG∘T

Interpretation

- ksoft effectively “scales down” the thermochemical barrier (ΔG°) because the lattice is easier to distort / mobilize when phonon modes are softened (i.e., the lattice has higher “compliance” under field).

- It is implicitly tied to the phonon softening physics (e.g., via reduced Ωq, increased Γ).

- We treat ksoft as an empirical family parameter (for rutile, fluorite, etc.) but its physical origin is the phonon softening / increased mode occupancy / lower restoring force captured by the unified phonon theory.

### 6. Field‐pumping of phonons (implicit)

In our ridge equation we have:

αres σT E2 e-γ

Interpretation in phonon terms

- Field E → current j=σE → Joule heating → increased phonon population / non-equilibrium phonons → extra “work” done on lattice modes.

- In phonon theory, this means higher phonon occupancy, more anharmonic scattering, possible mode softening (reducing Ω), and higher damping (Γ).

- So one could map this to an increase in Γω or decrease in Ωq via increased “pump” energy.

- αres = coupling coefficient linking electrical dissipation to effective phonon work.

- σT = electrical conductivity (S/m) of the material at T.

- E = applied field (V/m).

- γ = damping exponent (empirical).

- This term offsets the effective Gibbs barrier (makes it easier for events to happen) by lowering effective barrier via phonon pumping. When you work from the unified phonon theory side, you’d see this as shifting phonon lifetimes or stiffness, hence you can justify this term’s existence physically.

### How to map them into our workflow

- Choose a phonon‐softening model (e.g., eq 2 above) to compute how Ωq reduces when the field or defect population rises; derive an effective “softening factor” ksoft.

- Use the damping expression (eq 3) to estimate changing lifetimes τ≈1/Γ. From that compute changes in κ (eqn 4) and foresee higher heating and weaker lattice.

- Use the VDOS expression (eq 1) to estimate how many low‐ω modes contribute (i.e., more soft modes → more phonon modes that can be pumped).

- Tie the field pumping term (eq 6) to the phonon scattering/softening — thus rationalizing our αres·σE² term.

- Insert these changes into our Flash balance: the thermochemical barrier ΔG° gets scaled by ksoft, the pumping term comes from field work + phonon activation, and resulting transport properties (D, σ, etc) follow via lowered barrier and higher scattering.

| # | Equation | Variables | Use |
| --- | --- | --- | --- |
| 1 | Dω≈A ω2ω2+Γ2ω | Dω,ω,Γω | VDOS deviation from Debye; boson‐peak / soft‐mode contribution. |
| 2 | Ω2q=v2q2+Δ2, Δ2=ω021-q2/q02 | Ωq,v,q,ω0,q0 | Phonon softening / crossover from acoustic to resonant regime; sets softness scale. |
| 3 | Γq∼Γ0+B qm | Γq,Γ0,B,m | Phonon linewidth vs wavevector; lifetime / scattering. |
| 4 | κ=13∫Cω vgω lω dω | κ,Cω,vgω,lω,τω | Thermal conductivity; links phonon spectrum to κ. |
| 5 | Softening factor: ksoft×ΔG∘ | ksoft,ΔG∘ | Empirical scaling of barrier due to lattice softening. |
| 6 | Field‐pump term: αres σT E2 e-γ | αres,σ,E,γ | Links field dissipation to phonon‐mode pumping / barrier reduction. |

# References

1. Cologna, M., Rashkova, B. & Raj, R. Flash sintering of nanograin zirconia in <5 s at 850°C. J. Am. Ceram. Soc. 93, 3556–3559 (2010).

2. Francis, J. S. C. & Raj, R. Influence of the field and the current limit on flash sintering at isothermal furnace temperatures. J. Am. Ceram. Soc. 96, 2754–2758 (2013).

3. Naik, K. S., Sglavo, V. M. & Raj, R. Flash sintering as a nucleation phenomenon and a model thereof. J. Eur. Ceram. Soc. 34, 4063–4067 (2014).

4. Ding, G., Ma, E. & Jiang, F. Unified theory of phonon in solids with phase diagram of non-Debye anomalies. Nat. Phys. (2025).

5. Baggioli, M. & Zaccone, A. Unified theory of vibrational spectra in hard amorphous materials. Phys. Rev. Research 2, 013267 (2020).

6. Chase, M. W. NIST-JANAF Thermochemical Tables, 4th ed. (American Institute of Physics, 1998).

7. Ellingham, H. J. T. Reducibility of oxides and sulphides in metallurgical processes. J. Soc. Chem. Ind. 63, 125–133 (1944).

8. Kröger, F. A. & Vink, H. J. Relations between the concentrations of imperfections in crystalline solids. Solid State Phys. 3, 307–435 (1956).

9. Smyth, D. M. The Defect Chemistry of Metal Oxides. (Oxford University Press, 2000).

10. Ding et al, Unified theory of phonon in solids with phase diagram of non-Debye anomalies, Nature Physics volume 21, 1911–1919 (2025)

11. Dong, Y., Qi, L., Alvarez, A., Li, J. & Chen, I.-W. Enhanced mobility of cations and anions in the redox state: The polaronium mechanism. Acta Mater. 232, 117941 (2022). https://doi.org/10.1016/j.actamat.2022.117941

12. Jo S, Kindelmann M, Jennings D, et al. Flash-induced defects in single-crystal 8YSZ characterized by TEM, XRD, and Raman spectroscopy. J Am Ceram Soc. 2024. DOI: 10.1111/jace.19915

Data availability

All data needed to evaluate the Flash balance are contained in the manuscript; additional data will be made available upon reasonable request.

# Code availability

Reference implementations of the Flash onset solver will be made available upon reasonable request.

# Competing interests

The author declares no competing interests.